MAGNETIC ORDERING IN THE DECORATED SQUARE KAGOMÉ LATTICE MAGNETS 
V.N.Glazkov1,*, Ya.V. Rebrov1,2, M.M. Markina3, A.F. Murtazoev3, P.S. Berdonosov3, A.N. Vasiliev3

1 P. Kapitza Institute for Physical Problems, Kosygin str. 2, 119334 Moscow, Russia
2 Faculty of Physics, HSE University, Myasnitskaya str. 20, 101000 Moscow, Russia
3 Lomonosov Moscow State University, Leninskie gory 1, 119991, Moscow, Russia

*glazkov@kapitza.ras.ru

Nabokoite family compounds ACu7(TeO4)(SO4)5B (A=Na, K, Cs, Rb; B=Cl, Br) are the example of decorated square kagomé lattice (SKL): six copper ions form 2D SKL layers, while seventh ion takes inter-layer position [1]. Both intra-layer and inter-layer exchange bonds are highly frustrated. As a result, all compounds of this family orders around 3-5 K, while Curie-Weiss temperature is about 150-200 K.

We have performed accurate absolute calibration of the ESR absorption in the paramagnetic phase (10 K<T<200 K) which revealed that broad (ΔB≈2 T) paramagnetic absorption corresponds to approximately 1/7 of all copper ions present. This observation can be interpreted as ESR response of the decorating inter-layer copper ions. 

Transformation of this paramagnetic absorption into antiferromagnetic resonance below the Neél temperature possibly reveals partial ordering of inter-layer copper ions, while SKL layers remain in the disordered spin-liquid state.

Antiferromagnetic resonance frequency-field dependences and temperature dependences of spin-wave gaps below the Neél temperature are qualitatively different for nabokoite compounds with light (Na, K) and heavy (Cs, Rb) alkali ions. Compounds with light alkali ions demonstrate a two-step magnetic ordering into a non-collinear phase, while their heavy-alkali-ions counterparts demonstrate convenient easy-axis collinear ordering. Presumably, this qualitative difference in the choice of the ordering pattern is a result of partial lifting of the exchange bonds frustration due to minute structure modification at (anti)segnetorelectric transition, observed earlier in light-alkali-ions compounds only [2]. 

The work was supported by RSF grant 22-12-00259-П.
[1] A.F. Murtazoev, K.A. Lyssenko, M.M. Markina et al. ChemPhysChem 24, e202300111  (2023); M.M. Markina, P.S. Berdonosov, T.M. Vasilchikova et al. Mat. Chem. Phys. 319, 129348 (2024)

[2] Ya.V. Rebrov, V.N. Glazkov, A.F. Murtazoev et al. JMMM 592, 171786 (2024) 
