MAGNETIC PROPERTIES OF microsized and nanosized PrF3 POWDERs 
A.M. Garaeva, A.S. Makarchenko, G.A. Dolgorukov, I.V. Romanova, B.M. Mukhamadullin, E.I. Boltenkova and E.M. Alakshin
 Kazan Federal University, Kazan, Russia

The PrF3 is a dielectric Van Vleck paramagnet. The Pr3+ ion has the electron structure 4f12. Due to the low symmetry of the PrF3 crystal field, the ground multiplet 3H4 is split into 9 singlets. The nucleus of the rare earth element has a non-zero nuclear spin 5/2 and this element compounds have nuclear magnetism. PrF3 can be used for the dynamic polarization of 3He nuclear spins [1]. The polarized system of nuclear spins of gaseous 3He is widely used in medicine for NMR tomography of the lungs [2,3].
Micro-sized PrF3 powder particles were obtained by crushing a single crystal and then sifting through a 45 μm sieve. Nanoparticles of PrF3 with a size of 56 × 34 nm were obtained by hydrothermal synthesis using a nitrate reaction [4]. Control of the chemical composition and confirmation of crystallinity was carried out by X-ray phase analysis on a Bruker D8 Advance Cu Kα diffractometer, λ=1.5418 Å. Based on photographs taken by transmission electron microscopy on a HitachiHT Exalens microscope, the shape and characteristic size of particles in the resulting powders were determined.
In this work, magnetizations of micro- and nano-sized PrF3 powders were investigated. Magnetic field (0-9 T) and temperature (5-300 K) dependences of magnetization were measured using the multifunctional system for measuring physical properties with a superconducting magnet PPMS-9.  A change in the magnetization of PrF3 nanopowder is observed compared to a microsized sample. An explanation for this phenomenon is proposed.
Also, ³He NMR in contact with nanosized PrF3 particles were studied. The measurements were carried out on the home-built NMR spectrometry [5]. The effect of a powder of magnetic PrF3 particles on the rate of longitudinal and transverse relaxation of helium-3 nuclei in the adsorbed layer, gas and liquid, and with adsorbed helium-4 was studied. The measurements were carried out at a temperature of 1.5 K in fields up to 800 mT. The mechanisms of magnetic nuclear relaxation are considered. A model that describing the nuclear magnetic relaxation of helium-3 in contact with PrF3 nanoparticles is proposed.
This work was financially supported by the Russian Science Foundation (Project No. 23-72-10039).
1. M. S. Tagirov., JETP Letters, 61, 652 (1995).


2. H.E. Moller, X.J. Chen, M.S. Chawla, et al., J.Magn. Res., 135, 133 (1998).

3. Nacher P. J., Poincaré Seminar, 159 (2007).

4. Alakshin E.M., Gabidullin B.M., Gubaidullin A.T., et al., arXiv preprint arXiv:1104.0208. (2011).

5. Dolgorukov G.A., Kuzmin V.V., Bogaychuk A.V., et al., Magn. Reson. Solids 20, 18206 (2018).
