HIGH-ENTROPY PEROVSKITE-LIKE OXIDE (BaCaSrLaNa)0.2FeO3: SYNTHESIS AND EPR MEASUREMENTS
R.F.Likerov1, I.V.Yatsyk1, R.M.Eremina1
1 Zavoisky Physical-Technical Institute, FRC Kazan Scientific Center of RAS, Kazan, Russia

High-entropy oxides (HEO) are considered suitable for thermoelectric applications [1] and outperform traditional thermoelectric materials, such as Bi3Te2 in case of high working temperatures. The following characteristics of HEO are important: thermal conductivity κ, electrical conductivity σ, Seebeck coefficient S. 

In this work, we report the synthesis and EPR study of Ba0.2Ca0.2Sr0.2La0.2Na0.2FeO3 HEO with perovskite-like structure. This compound was synthesized by solid-state reaction method. We used analytical grade reagents such as BaCO3, CaCO3, SrCO3, Na2CO3, La2O3 and Fe2O3 (all are >99% purity), which was mixed in planetary ball mill at 300 rpm for 3 hours. Then we calcined mixed powders in air for 6 hours at T = 1050°C and pressed calcined powders with P = 470 MPa for pellet sintering at T = 1100°C for 6 hours. 

Room temperature CW EPR measurements at X-band showed magnetic phase stabilization for Ba0.2Ca0.2Sr0.2La0.2Na0.2FeO3 sintered pellet in comparison with calcined powders (figure 1). 
	
[image: image1.emf]0 200 400 600 800 1000 1200 1400 1600

d

c

"/dB (arb. units)

B (mT)

 Initial powder

 1050°С

 1100°С

T=297 K

(BaSrCaLaNa)

0.2

FeO

3



	Fig. 1. Room temperature EPR spectra of initial precursor powders (black line), calcined powders (red dash line) and sintered pellet formed by pressurizing the calcined powders (blue dash-dot line).


1. Bhattacharya T., Banerjee R., Maiti T.: Phys. Chem. Chem. Phys., 26, 28874-28883 (2024) 
_1811864983.bin

