MEASURING MAGNETOSTRICTION USING CAPACITIVE DILATOMETER

M.E. Menshikov1, A.V. Dooglav1, R.G. Batulin, S.L. Korableva,

 O.A. Morozov, I.V. Romanova1
1 Kazan Federal University, Kazan 420008, Russia

In this paper, we present the construction of capacitive dilatometer and the results of measuring the magnetostriction of the Van Vleck dielectric single crystal of lithium-thulium double fluorides LiTmF4 along the [100] crystallographic axis. The capacitive dilatometer was designed and assembled according to the design proposed by G. M. Schmiedeshof et al [1] and was used with a PPMS system and a capacitive bridge [2].

The LiTmF4 single crystal was grown by S. L. Korableva using the Bridgman-Stockbarger method. After evaluating the single crystallinity and axis orientation, two parallel planes perpendicular to the crystallographic axis [100] were selected and polished using a brass mandrel and water-based abrasives.

Using a capacitive dilatometer, the magnetostriction of the LiTmF4 single crystal was obtained at a temperature of T = 5 K. A single crystal LiTmF4 was selected as a reference sample for the study. Our data are consistent with previous studies by Altshuller and Krotov in 1980 up to 3 T [3] and also qualitatively consistent with preliminary calculation in a single crystal up to 3.5 T.

This work was supported by RSF grant #22-12-00259-П
1. Schmiedeshoff G. et al. Rev. of Sci. Instrum 77.12 (2006).

2. Model 2550A digital capacitance bridge manufactured by Andeen-Hagerling, Inc.

3. Al’tshuler S., Krotov V., Malkin B. JETP Lett. 32(3), 232-235 (1980)

