HYPERFINE STRUCTURE OF EPR SPECTRA OF Cr-53 IMPURITY IONS IN SYNTHETIC FORSTERITE
A.A. Sukhanov1, V.F. Tarasov1, Ya.S. Didenko2, K.A. Subbotin3, 
E.V. Zharikov2 
1 Zavoisky Physical-Technical Institute, FRC Kazan Scientific Center of RAS, Kazan, Russia
2 Prokhorov General Physics Institute of the Russian Academy of Sciences, Moscow, Russia
Single crystals of synthetic forsterite (Mg2SiO4) doped with chromium ions are known as effective laser media for generation of femtosecond pulses in the range of 1230-1580 nm. The active laser centers are Cr4+ ions substituting Si4+ ions in tetrahedral positions. At the same time, Cr2+ and Cr3+ ions can substitute Mg2+ in the forsterite crystal lattice.
In this work we studied hyperfine structure (HFS) of continuous wave EPR spectra of Cr2+ and Cr3+ ions substituting Mg2+ ions in two structurally nonequivalent octahedral positions M1 and M2. Crystal was grown from the melt with 0.14 wt. % Cr by the Czochralski technique in slightly oxidizing atmosphere. The 53Cr isotope content was 0.977 %. Measurements were carried out in X-band at temperatures of 80 and 300 K on Bruker ELEXSYS E680 spectrometer. 

Two different types of HFS were detected. The HFS of a single 53Cr3+ ion, shown in Fig. 1a, consists of 4 lines corresponding to allowed transitions between nuclear levels of the 53Cr with nuclear spin I = 3/2. A weak signal from even chromium isotopes is observed in the center of the spectrum. In addition to these spectra, spectra with a more complex HFS were detected. An example of such a spectrum is presented in Fig. 1b. We believe that this spectrum is due to a 53Cr3+-53Cr3+ dimer associate. In general, the HFS of this associate should consist of 16 allowed transitions, however, some lines overlap each other. Therefore, the HFS represents 7 lines corresponding to the total nuclear spin Idim = 3 with a ratio of intensities of 1:2:3:4:3:2:1. 
[image: image1.png]225 230 235 240

440 445 450 455 460
Magnetic Field (mT)





Fig. 1. Spectra of 53Cr3+ ions in Mg2SiO4. a – single Cr3+ ion; b - Cr3+-Cr3+ dimer associate.
